## Slide 1: Summary of Beaune 2005
University of California, Los Angeles
Department of Physics and Astronomy
arisaka@physics.ucla.edu
Katsushi Arisaka

## Slide 2: Outline
Focus on big picture:
  New trend on scientific applications
  Demands, specs on detectors
  Major new technology
  Fair comparison of detectors
My apologies for not including:
  UV, X and direct Gamma detection
  Readout electronics, systems
  Friday’s talks

## Slide 3: Why are we here?
F. Rocard

## Slide 4: Are we alone?
F. Rocard

## Slide 6: Science of 21st Century
Why are we here?
  Origin of Ourselves
  Origin of Life
  Origin of the Solar System
  …
  Origin of the Universe
What is the most fundamental law in nature?
We rely on weak, fast photon signals.

## Slide 7: Scientifics Applications
High Energy
Particle Astrophysics
Bio and Medical Imaging

## Slide 8
High Energy
LHC
B-Factory etc.
ILC

## Slide 9: Large Hadron Collider (LHC)
Expected to start in 2008.

## Slide 10: CMS Detector under 4 Tesla
4 Tesla
EM
Hadron
APD
HPD

## Slide 11: APD’s for CMS ECAL (HPK) (Beaune 2002)
Today’s APD is a result of about 10 years R&D with (EG&G and) Hamamatsu Photonics KK.
Delivery from Hamamatsu started last year: ~37 000 APD`s delivered so far

## Slide 12
CMS HCAL Multi pixel HPD (DEP)
(Beaune 2002)
PIN Diode
array
Ceramic feedthrough
Fiber-Optic
Window
Photocathode (-10 kV)
e
19 channel pixel layout
pixel size: 5.4 mm flat-flat
gap between pixels: 0.04 mm
3.4 mm

## Slide 13: LHCb experiment
T. Gys

## Slide 14
The pixel HPD by DEP
Advantages of this hybrid, pixel structure:
low noise: excellent resolution of single photoelectrons
high channel number/density
DEP, The Netherlands
K. Wyllie

## Slide 15: Belle Spectrometer - PID
Particle identification:
TOF
dE/dx
ACC: threshold aerogel Cherenkov counter
Large solid angle detector
at the KEKB e+ e- collider
P. Krizan

## Slide 16: COMPASS at CERN
D. Neyret

## Slide 17: International Linear Collider
Electron/Positron collider .
Expandable, energies 0.5TeV to 1.5TeV.
10X larger than the Stanford Linear Accelerator.
Two detectors.

## Slide 18: ILC Detector Concepts
2Tesla
5Tesla
D. Chakraborty

## Slide 19
Particle Astrophysics
(Eckart Lorenz)

## Slide 20: Multi-Messenger Exploration of Energy Frontiers
Energy Frontier of Particle Physics, Cosmology and Astronomy
  Earliest Universe: Inflation, Planck Scale …
  Extreme Universe: AGN, GRB, SN …
Need for Multi-Messenger Approach
  Gamma ray Hess, MAGIC, GLAST …
  Charged Particle Auger, EUSO …
  Neutrino Super-K, Icecube…
  Gravitational Wave LIGO, VIRGO, LISA …
  Anti-Matter AMS, BESS…
  Dark-Matter CDMS, Edelweiss …

## Slide 21: Super-Kamiokande
11,200 of 20” PMTs

## Slide 22: Hyper Kamiokande, UNO
H. Nakayama

## Slide 23: ICECUBE
1 km
  60 PMTs/string x 80 strings
  = 4,800PMTs

## Slide 24
AMS - Anti-Matter Search
G. Paic

## Slide 25: EUSO on International Space Station
EUSO
A. Petrolini

## Slide 26: EUSO Detector
2.5m Diameter
60o FOV
f/1.25
Hamamatsu
R7600-M36
250k Pixel
A. Petrolini

## Slide 27: Detection of Cosmic Radiation
CDMS
Super-K
AMANDA
Pierre-Auger
Hyper-K
ICECUBE
EUSO
OWL
Zeplin
Larger Volume
Lower Threshold
Dark Matter
Neutrino
Cosmic Ray

## Slide 28: Photon Detector
SDSS
EUSO
VERITAS
Super-K
LSST
OWL
 Wide FOV
Hyper-K
More Pixels
Better Sensitivity
CCD
PMT
Auger-FD
Auger-SD
AMS

## Slide 29
Bio/Medical Imaging
SPECT & PET
Molecular Imaging

## Slide 30: g-Camera Today
Workhorse of nuclear medicine
http://www.is2research.com/
Improvements:
  Large imaging area (up to 91 PMTs)
  Square & rectangular imaging FOV
  Variety of configurations for specific needs
  Digital signal processing  improved E & x
  Multiple heads
  Rotating gantry for tomography (SPECT)
99mTc Sestamibi 64  64 matrix 48 45-sec steps
Gated 8 frames/R-R
HRGP Collimator (250 cpm/µCi)
512 x 512 HRLE Collimator (190 cpm/µCi)
Bone scan
Cardiac SPECT imaging
R. Lecomte

## Slide 31
Anger Camera
Inexpensive
Isotropic spatial resolution
  ~5 mm FWHM
High energy resolution
  Efficient scatter rejection
Poor stopping power
Limited count rate / high dead time
Excellent spatial resolution possible by reducing crystal thickness at the expense of sensitivity (Green et al)
Count rate performance can be improved by:
  Local triggering
  Slotted surface / Detector granularity
  Faster scintillator
Large continuous NaI(Tl) bars
C-PET Module
Adam et al, J Nucl Med 42:1821-30, 2001
R. Lecomte

## Slide 32: Crystals
Crystals | Density (g/cm3) | Light yield (ph/MeV) | Decay time (ns) | Maximum Emission lenght (nm) | E/E (FWHM) PMT read-out | 
 |  |  |  |  | 662 keV ** | 140 keV
NaI:Tl | 3.67 | 41000 | 230 | 410 | 5.6 % | 8.5 %
CsI: Na | 4.51 | 40000 | 630 | 420 | 7.4 % | 9.5 %
CsI:Tl | 4.51 | 66000 | 8006103 | 550 | 6.6 (PMT)/ 4.3 (SDD) | 14 %
LaCl3 :Ce | 3.79 | 49000 | 28 | 350 | 3.8 % | 8.0* %
LaBr3 :Ce | 5.3 | 63000 | 26 | 380 | 2.8 % | 5.8 %
Bi4Ge3O12 (BGO) | 7.1 | 9000 | 300 | 480 | 9.0 % | --
Lu2SiO5:Ce (LSO) | 7.4 | 26000 | 40 | 420 | 7.9 % | 18 %
Gd2SiO5:Ce (GSO) | 6.7 | 8000 | 60 | 440 | 7.8 % | 22 %
YAl O3:Ce (YAP) | 5.5 | 21000 | 30 | 350 | 4.3 % (APD) | 20 %
** from C.W.E. van Ejjk Phys. Med. Biol. (2002) 85-106 * Expected values |  |  |  |  |  | 
R. Pani

## Slide 33
Good packing fraction
Poor light collection
Individual Coupling & Independent Processing
Munich APD PET (MADPET II)
PTFE
LSO
APD array
3M foil
4  8 APD Array (Hamamatsu Photonics)
2  2  6 mm3 LSO individually coupled
b ~ 0 mm  Intrinsic FWHM ~ 1.2 mm
Pichler et al,
IEEE MIC 2000
R. Lecomte

## Slide 34
Dual APD Readout
PS-APD Module
1.65  1.65  22 mm3 MLS crystals
8  8 array on dual 14  14 mm2 PS-APDs
~ 3 mm FWHM DOI resolution
Burr et al, IEEE NSS/MIC 2003
R. Lecomte

## Slide 35
Intrinsic Spatial Resolution of PET Scanners
R. Lecomte

## Slide 36: Nutts’ Law
R. Lecomte

## Slide 37
The H33D detector attaches to a standard fluorescence microscope
H33D
Laser
It will permit to track multicolor qdot-labeled proteins in live cells virtually background-free
The H33D capabilities will allow protein-protein interaction, protein trafficking at the single-molecule level to be followed with nanometer resolution and arbitrary time-resolution
Single Molecule Imaging
X. Michalet

## Slide 38: Emission of Quantum Dot
CdSe
InP
InAs
2.1nm
4.6nm

## Slide 39
Schematic of the H33D detector
MCP 1
…
MCP n
Photocathode
XDL or XS Anode
h
n
e
-
e
-
cloud
X
Y
t (100 ps) + T (20 ns)
~ ps
Sample excitation
(Laser)
Sample emission
(dye, quantum dot)
~ ns
X + Y + T = 3D
High spatial resolution: 100 um
High temporal res. : 100 ps
High throughput: 50 MHz
= H3
H33D = Heed = Attention, Notice
X. Michalet

## Slide 40: General Requirements
Various Sizes
  Large Area > 30 cm
    Neutrino, Proton decay…
  Coarse Pixel 1-5 mm
    RICH, Tile Calorimeter, EUSO, PET…
  Imaging < 100 m
    Astronomy, Single Molecule…
High Speed
  TTS < 1 nsec
  Rate > 1 MHz
Single Photon Counting
(Insensitive to Magnetic Field)
Los Cost !

## Slide 41: New Developments on Detectors
Gaseous
PMT
Hybrid
Solid State

## Slide 42
Gaseous Detector
(Amos Breskin)

## Slide 43
CERN-ALICE CsI-RICH
Single arm detector, radial distance of 4.9 m
|h| < 0.9, 5% of barrel acceptance
Proximity focusing (80 mm gap), 15 mm C6F14
radiator, 7 modules each with 6 CsI PC
Total active area ~12 m2
FEE: Gassiplex 0.7 m, noise 1000 e-
HMPID 1st MODULE!
~2m2
CsI-RICH:
ALICE, HADES, COMPASS, J-LAB….
ALICE-RICH: 12m2
RICH: Ring Imaging Cherenkov UV-detectors for particle identification
1 element: 400 x 600 mm2
Amos Breskin

## Slide 44: COMPASS RICH
D. Neyret

## Slide 45
Gated GPM for visible light
A. Breskin et al. Physics/0502132
GAIN: 100-1000 in DC mode (ion feedback limit)
~106 in ion-gating mode
A breakthrough!
Ion gating
DC
Amos Breskin

## Slide 46
+
R-MHSP
C
A
Ion Back-flow Reduction: Reversed-MHSP
R-MHSP: hole-gain & ion defocusing
from successive multiplier*
MHSP: 2-step gain & some ion blocking
* R-MHSP: Roth, Vienna 04
Simulations:Oleg Bouianov
Ion blocking:
Breskin et al. physics/0502132
Veloso et al. physics/0503237
Amos Breskin

## Slide 47: A Very Flat Gaseous Imaging PM
~10mm
hn
photocathode
THGEM
readout
100x100mm2 THGEM
With 2D delay-line readout
f 0.3mm holes
Amos Breskin

## Slide 48
Photomultiplier
High QE Alkali
Multi Pixel, Flat PMT

## Slide 49: Hamamatsu High QE Photocathode
Bialkali Photocathode
new process BEST | 37 %
new process TYPICAL | 34 %
standard typical | 27.5 %
0
5
10
15
20
25
30
35
40
200
300
400
500
600
700
800
Wavelength [nm]
Quantum Efficiency [%]
ＮaＩ(Tl)
ＢＧＯ
New Process
Standard
(at 360 nm)
Hamamatsu / Y Yoshizaawa

## Slide 50
Improved QE of Photonis 9 inch PMT
UV
Quantum efficiency (600 nm)
- Standard: ~1.6%
- Improved: ~6.3%
+ 75%
Extension of the spectral sensitivity in the red region
Quantum efficiency (400 nm)
- Standard: ~26%
- Improved: ~32%
+ 19%
D. Dornic

## Slide 51: Hamamatsu Flat Panel PMT
3 x 3 array
H8500 (2 inch square)
Pixel Size : 6 x 6 mm
500 tubes were delivered since 2002
for Medical, Radiation monitor and HEP.
Hamamatsu / Y. Yoshizaawa

## Slide 52: Burle Flat MCP PMT
BURLE 85011 MCP-PMT:
multi-anode PMT with 2 MCPs
25 mm pores
bialkali photocathode
gain ~ 0.6 x 106
collection efficiency ~ 60%
box dimensions ~ 71mm square
64(8x8) anode pads
pitch ~ 6.45mm, gap ~ 0.5mm
active area fraction ~ 52%
P. Krizan

## Slide 53
Hybrid Detector
GaAsP HAPD
Multi Pixel
Large Area

## Slide 54: HPD with 18-mm GaAsP Photocathode by Hamamatsu
Designed for MAGIC-II camera
Photocathode | GaAsP (for high QE)
Cathode Size | 18 mm [old < 8 mm]
Avalanche Diode | 3 mm Silicon
Sensor shape | hexagonal 28 mm
 | 39 mm height
<Parameters>
M. Hayashida

## Slide 55: QE of GaAsP + WLS
M. Hayashida

## Slide 56
D
V
photocathode
focusing
electrodes
silicon
sensor
+ FE
electronics
e
-
light quantum
segmented
silicon
sensor
Gain:
Gain is achieved in a single
dissipative step !
UC = 20 kV  G ~ 5000
Hybrid Photon Detectors (HPD)
C. Joram

## Slide 57: DEP Hybrid Photodiode (HPD) (Beaune 2002)
Baseline design for LHC-b RICH
8cm diameter
61 Pixel, (5mm view)
T. Gys

## Slide 58: HPD pre-series (9 tubes): performance results
Item | Specification | Results
Pixel response | >95% | >99%
Min. threshold Noise | <2000e- <250e- | Typ. 1200e- Typ. 160e-
Leakage current | Typ. 1uA @ 80V bias | < 1uA
Dark count rate | Max. 5kHz/cm2 | 0.03–3kHz/cm2
Ion feedback rate | Max. 10-2 rel. to signal | <10-3
P.e. detection efficiency | Typ. 85% | 79-89%
Quantum efficiency | See next picture | Generally well above specs
T. Gys

## Slide 59: Multi-pixel HAPD (8x8 matrix)
16mm
16mm
8x8 Matrix (64 Pixels)
2x2 mm / Pixel
APD Format
43mm in diameter
15
mm
FOP with Multialkali
R9503U-04-M064
Effective Area
Hamamatsu / Y. Yoshizaawa

## Slide 60: RMD Position Sensitive HAPD
Proximity design
14 x 14 mm2 PSAPD
High gain 106 to 107
320 m with ~5 photons/pulse
8 x 8 CsI:Tl, 1 mm pixel CsI:Tl imaged at 23 °C with 241Am (60 keV).
M. McClish, K.S. Shah, R. Grazioso, J. Glodo, R. Farrell, E. Karplus, R. Benz, “A hybrid position sensitive avalanche photodiode detector for scintillation spectroscopy and imaging,“ IEEE NSS Conf. Rec. Oct. 19-25, 2003, Portland, OR.
RMD / M. McClish

## Slide 61: 13inch HAPD by Hamamatsu
 | 13inch | 5inch
Diameter | 332mm | 128mm
Effective area | 240mmf | -
APD size | 5mmf | 3mmf
APD type | Low capacitance (~70pF) | Low capacitance (~30pF)
Bias max | 370V | 350V
HV max | +12kV | -8.5kV
H. Nakayama

## Slide 62
HPD developed and built at CERN
NIM A 442 (2000) 128-135
NIM A 478 (2002) 400-403
www.cern.ch/ssd/HPD
5-inch  10-inch
127 mm Ø, D ~ 2.5,
2048 channels 1mm2
bialkali photocathode
NIM A 504 (2003) 19
NIM A 518 (2004) 574-578
254 mm Ø, D ~ 4,
2048 channels 1mm2
bialkali photocathode
C. Joram

## Slide 63
Al coating
2 rings
C2GT Optical Module (38cm)
C. Joram

## Slide 64: Development of Other Vacuum Devices
~1960
~2000
Production Cost: < $1,000 per m2
D. Ferenc

## Slide 65: Light Amplifier Concept
Scintillators + fiber optics
APD array
READOUT 
Resolution determined outside !!
NO electronics in the vacuum
D. Ferenc

## Slide 66
Solid State Detector
APD
SiPM

## Slide 67: Planar Process for APD Fabrication
Deep Diffusion
into Si wafer,
p-n-p
Si Removal
Bevel Formed
HV
Wafer Diced
HV
Standard Wafer
Grooved Wafer
R. Farrell, K.S. Shah, K. Vanderpuye, R. Grazioso, R. Myers, G. Entine “APD arrays and large-area APDs via a new planar process,” Nuc. Inst. Meth. Phys. Res. A, Vol. 442, pg. 171, 2000.
RMD / M. McClish
Notes: Mention manual beveling being tedious and causing high cost.
Mention grooved wafer, affecting doping profile, surface passivation, diced and plated with electrodes.

## Slide 68: Position Sensitive and Discrete APDs
45 cm2 Planar APD
8 x 8 mm2 PSAPD
RMD / M. McClish

## Slide 69: Fabrication for Position Sensitivity
-HV
K.S. Shah, R. Farrell, R. Grazioso, E. Harmon, E. Karplus, “Position-sensitive avalanche photodiodes for gamma-ray imaging,” IEEE Trans. Nuc. Sci., Vol. 49, No. 4, August 2002
RMD / M. McClish
Notes: Mention how algorithm causes a pin cushion distortion, but can be corrected in software or using a look-up table.

## Slide 70: RMD APD for PET Applications
28 x 28 mm2 PSAPD coupled to 7 x 7 LSO array with 3 mm pixels at –20 °C. Average energy resolution = 15.5% at 511 keV.
CHANNELS
COUNTS
8 x 8 mm2 PSAPD coupled to 6 x 6 LSO array with 1 mm pixels at 23 °C. Average energy resolution = 16% at 511 keV.
COUNTS
RMD / M. McClish
Notes: Mention image distortion and how cooling is needed for larger devices due to their increased noise from increased current leakage.

## Slide 71: Silicon Photomultiplier (from Beaune 2002)
Gain~106
DQE~10%
ENF=1.0
P. Buzhan, B. Dolgoshein et. al.

## Slide 72
At present many people consider that the new APDs with
inner microstructures are very easy devices. To my mind, the way to micro-pixel APDs was not easy. This development took about 20 years.
Different generations of silicon avalanche structures produced in 1983-2005.
MOS and MRS type APDs.
1983-1993.
MRS and CCD type APDs.
1994-2001.
CCD and MW type APDs.
2002- present
Long History of SiPM
Z. Sadygov

## Slide 73: Various SiPM
Y. Musienko, V. Saveliev

## Slide 74: SiPM Layout
General view 1x1 mm,
Common Electrode Layout,
Microcells with Quenching Mechanism,
Pulsar SiPM
(LCWS2004, M.Danilov ITEP,Moscow )
CPTA SiPM
V. Saveliev

## Slide 75: PE Distribution of Various SiPM
Y. Musienko

## Slide 76: SiPM Performance
Detection Efficiency – Wavelength Dependent:
is limited by dead layers on the top of structure
is limited by the thickness of sensitive layer of SiPM
QE of Hamamatsu Photonic APD
Efficiency of Si-PM
UV region of SiPM
IR region of SiPM
The Si-PM has green light sensitivity
and total Detection Efficiency for green range of light is ~25%
Thickness of Sensitive Layer
Thickness of Dead Layer
Geometry
Absolute value scaling
is limited by geometry factor
V. Saveliev

## Slide 77: QE of Various SiPM
Y. Musienko
Reference PMT

## Slide 78
B.Dolgoshein
32 m
64 m
96 m
128 m
Optical Cross Talk of 1mm2 SiPM

## Slide 79
Dark Rate of 1mm2 SiPM
B.Dolgoshein
1 MHz / mm2

## Slide 80: Future of SiPM
Combination of the Sensors and FE Electronics in the same technology Process.
(IEEE STQE, v10, Jul-Aug, 2004,C.Niclass)
V. Saveliev

## Slide 81
Larger area (up to 10x10 mm2) is required for a number of applications:
astroparticle physics
PET
Particle physics
. . .
SiPM 3x3 mm2, 5625 pixels
B.Dolgoshein
Large Area SiPM

## Slide 82: SiPMs in ILC Tile HCAL Prototype
SiPMs
1156 pixels
1x1 mm2
Precise ceramic plate
5±0.03
3
Tile with milled groove for WLS and precise hole for SiPM installation
The first HCAL prototype cassette
40 Cassettes will be required
E. Popova

## Slide 83
Production for ALICE CRF
Akindinov et al., High-efficiency and low noise scintillation detector for ionizing particles START (Scintillation Tile with MRS APD Light ReadouT)
A. Akindinov

## Slide 84
Space experiment “LAZIO”(MEPHI-INFN Collaboration)
SiPM’s in space ! International Space Station: launched by 15th of April,2005
Latitude particle flux dependence
Scientific goal:The measurement of low energy particle fluxes and radiation monitoring by apparatus,including sci tile+WLS fiber+SiPM hodoscope system
B.Dolgoshein

## Slide 85: Final Comparisons
QE
TTS
Energy Resolution
Cost

## Slide 86: Quantum Efficiency (Beaune 1999 )
K. Arisaka
 2002
GaAs-Blue
GaAs
 2005
Bi-Alkali
SiPM

## Slide 87: Time Resolution vs. Sensitive Area (Beaune 1999 )
K. Arisaka
 2005
HPD
SiPM

## Slide 88: Effect of Magnetic Fields (Beaune 1999 )
Metal
Channel
Fine
Mesh
MCP
PMT
Solid
State
Linear
Focus
K. Arisaka
 2005
HPD
APD
SiPM
CMS

## Slide 89: Equivalent Noise Charge (ENC) after CRRCn
A useful formula : ENC (e- rms) after a CRRC2 shaper :
  en in nV/ √Hz, in in pA/ √Hz are the preamp noise spectral densities
  Ctot (in pF) is dominated by the detector (Cd) + input preamp capacitance (CPA)
  tp (in ns) is the shaper peaking time (5-100%)
ENC = 174 enCtot/√tp (δ)  166 in√tp (δ)
Noise minimization
  Minimize source capacitance
  Operate at optimum shaping time
  Preamp series noise (en) best with high trans-conductance (gm) in input transistor
  => large current, optimal size
C. De La Taille

## Slide 90: Energy Resolution (/E)
In ideal case:
In reality:
      N Number of incident photons
      QE Quantum Efficiency
      CE Collection Efficiency:
      ENF Excess Noise Factor (from Dynodes)
      ENC Equivalent Noise Charge (Readout Noise)
      G Gain
K. Arisaka

## Slide 91: Summary Table (Beaune 1999)
 | QE | CE | i | ENF | G | ENC | /E
Ideal | 1.0 | 1.0 | 1000 | 1.0 | 106 | 0 | 1/N
PMT | 0.25 | 0.9 | 10 | 1.3 | 106 | 1000 | 5.8/N
PD | 0.7 | 1.0 | - | 1.0 | 1 | 1000 | 1.4/N+(1400/N)2
APD | 0.7 | 1.0 | 2 | 2.0 | 100 | 1000 | 2.9/N+(14/N)2
HPD | 0.25 | 0.9 | 1000 | 1.0 | 103 | 1000 | 4.4/N+(4.4/N)2
HAPD | 0.25 | 0.9 | 1000 | 1.0 | 105 | 1000 | 4.4/N
VLPC | 0.7 | 1.0 | 1000 | 1.0 | 105 | 1000 | 1.4/N
K. Arisaka

## Slide 92: Summary Table (Beaune 2005)
 | QE | CE | i | ENF | G | ENC | /E
Ideal | 1.0 | 1.0 | 1000 | 1.0 | 106 | 0 | 1/N
PMT | 0.35 | 0.9 | 10 | 1.3 | 106 | 200 | 3.8/N
PD | 0.7 | 1.0 | - | 1.0 | 1 | 200 | 1.4/N+(280/N)2
APD | 0.7 | 1.0 | 2 | 2.0 | 100 | 200 | 2.9/N+(2.9/N)2
HPD | 0.5 | 0.9 | 1000 | 1.0 | 103 | 200 | 2.2/N+(0.4/N)2
HAPD | 0.5 | 0.9 | 1000 | 1.0 | 105 | 200 | 2.2/N
SiPM | 0.7 | 0.4 | 1000 | 1.3 | 106 | 1000 | 4.3/N
VLPC | 0.7 | 1.0 | 1000 | 1.0 | 105 | 200 | 1.4/N
K. Arisaka

## Slide 93: Resolution (over Poisson Limit) (Beaune 1999)
HPD
APD
K. Arisaka
PMT
Hardon
Calorimeter
TOF
RICH
EM Calorimeter

## Slide 94: Resolution (over Poisson Limit) (Beaune 1999)
PMT
HPD
APD
PD
HAPD
VLPC
K. Arisaka

## Slide 95: Resolution (over Poisson Limit) (Beaune 2005)
PMT (35% QE)
HPD (50% QE)
APD
PD
HAPD
VLPC
K. Arisaka
SiPM
G-APD

## Slide 96: Market Price (Beaune 1999 )
K. Arisaka
 2005
SiPM?
Silicon
HPD?

## Slide 97
Katsushi’s Dream Detector
(at Beaune 1999, 2002)
Glass Window (1mmt)
50.5mm
Solid State Photo Cathode
APD Array
Readout Electronics
47.6mm
Ceramic Case
(32 x 32 = 1024 Pixel)
HV
LV
Optical Fiber for
Signal Readout
1.4mm Pixel Size
32 x 32 = 1,024 Pixels
QE ~ 50% at 350 ~ 500nm
Gain ~105

## Slide 98
Katsushi’s Dream Detector
(at Beaune 2005)
Glass Window (1mmt)
52.5mm
Solid State Photo Cathode
APD Array
Readout Electronics
50.2mm
Ceramic Case
(1024 x 1024 = 1M Pixel)
HV
LV
Optical Fiber for
Signal Readout
50 m Pixel Size
1024 x 1024 = 1M Pixels
QE ~ 80% at 300 ~ 800 nm
Gain ~105

## Slide 99: Concluding Remarks
Areas of interests at Beaune 2005:
  SiPM
  Large area HPD
  Integrated front-end electronics
Future direction will be driven by
  Broader markets (outside of Physics)
  Low Costs